## Slide 1
Machine learning techniques for high-throughout analyses of TR-PES measurements
Convolutional Neural Networks employed to fit XPS spectra
Romaric Sallustre, Arthur Julien, Jean-Baptiste Puel, Philip Schulz
22/05/2024

## Slide 2
Objective: high throughput fits of XPS spectra
Two different chemical environments for nitrogen atoms
Two different contributions in mixed composition
Fitting procedure must allow to distinguish peak contributions in XPS spectra
Jacobsson, T. J., Correa-Baena, J. P., Halvani Anaraki, E., Philippe, B., Stranks, S. D., Bouduban, M. E. F., Tress, W., Schenk, K., Teuscher, J., Moser, J. E., Rensmo, H., & Hagfeldt, A. (2016). Unreacted PbI2 as a Double-Edged Sword for Enhancing the Performance of Perovskite Solar Cells. Journal of the American Chemical Society, 138(32), 10331–10343.
1000 spectra to analyze
TR-XPS measurements: high throughput analysis methods are necessary

## Slide 3
Convolutional neural networks for iterative identification of major peak
Convolution neural networks: serial connection of convolution products and filters
Park, S. H., Park, H., Lee, H., & Kim, H. S. (2021). Iterative peak-fitting of frequency-domain data via deep convolution neural networks. Journal of the Korean Physical Society, 79(12), 1199–1208.
Principle of the procedure: iterative identification of , and for each peak contribution.
Outputs of the CNN: parameters of the peak with largest area:
Fitting parameters:
: peak position
: peak width
: peak amplitude

## Slide 4
Results on experimental TR-XPS measurements
Total fit time (100 spectra): 43 sec
Filtering noisy experimental data
4f 5/2
4f 7/2
Laser off
Laser on
(eV)

## Slide 5
Perspectives
I 3d 5/2
Pb 4f
(eV)
(eV)
Possibility to track supplementary smaller contributions:
Park, S. H., Park, H., Lee, H., & Kim, H. S. (2021). Iterative peak-fitting of frequency-domain data via deep convolution neural networks. Journal of the Korean Physical Society, 79(12), 1199–1208.
Pielsticker, L., Nicholls, R. L., DeBeer, S., & Greiner, M. (2023). Convolutional neural network framework for the automated analysis of transition metal X-ray photoelectron spectra. Analytica Chimica Acta, 1271.
Adapt models and training to specific peaks identifications
Directly detect several peaks (vs iterative approach)
Detect pairs of 5/2 – 7/2 peaks
Combine existing / develop new architectures