## Slide 1
Machine learning techniques for high-throughout analyses of TR-PES measurements
Convolutional Neural Networks employed to fit XPS spectra
Arthur Julien, Jean-Baptiste Puel, Philip Schulz
18/03/2024

## Slide 2
Context: time resolved XPS measurements
Objective of the experiment: quantify changes of material properties upon illumination
1000 XPS spectra to analyze
Laser on
Laser off
Laser on
Laser off
High throughput analysis methods are necessary

## Slide 3
Objective: high throughput fits of XPS spectra
Two different chemical environments for nitrogen atoms
Two different contributions in mixed composition
Fitting procedure must allow to distinguish peak contributions in XPS spectra
Jacobsson, T. J., Correa-Baena, J. P., Halvani Anaraki, E., Philippe, B., Stranks, S. D., Bouduban, M. E. F., Tress, W., Schenk, K., Teuscher, J., Moser, J. E., Rensmo, H., & Hagfeldt, A. (2016). Unreacted PbI2 as a Double-Edged Sword for Enhancing the Performance of Perovskite Solar Cells. Journal of the American Chemical Society, 138(32), 10331–10343.

## Slide 4
Iterative identification of major peak
Model to fit each peak contribution: pseudo-Voigt profile (sum of Gaussian and Lorentzian functions):
Ratios between both functions are fixed (, and )
Fitting parameters:
: peak position
: peak width
: peak amplitude
Principle of the procedure: iterative identification of , and for each peak contribution.
Park, S. H., Park, H., Lee, H., & Kim, H. S. (2021). Iterative peak-fitting of frequency-domain data via deep convolution neural networks. Journal of the Korean Physical Society, 79(12), 1199–1208.
Convolutional neural networks
Procedure proposed by Park et al. in: Iterative peak-fitting of frequency-domain data via deep convolution neural networks. Journal of the Korean Physical Society, 79(12), 1199–1208.

## Slide 5
Convolutional neural networks
Principle of convolution neural networks: serial connection of convolution products and filters
Convolution layer: convolution with a kernel
Parameters that are optimized during training
Filtering / subsampling layer:
Max pooling
Fully connected layer:
All inputs are connected to outputs
Weights of the connections are optimized during training

## Slide 6
Convolutional neural networks for peak identification
Input: 1D vector containing one XPS spectrum
Outputs: four values:
Major peak position
Major peak width
Major peak amplitude
Total number of peaks
Convolution layer
Filtering layer
Contemporary CNNs include now significantly more layers:
Activations functions
Normalizations
Random perturbations
…
Training of CNN is necessary to adjust internal parameters and obtain desired outputs

## Slide 7
Training CNNs
Total spectrum | Major peak position | Major peak width | Major peak amplitude | Total number of peaks
. . . |  |  |  | 
 | 4.51 | 0.87 | 0.94 | 4
. . . |  |  |  | 
Input of CNN
Internal parameters of CNN are optimized to minimize error between CNN outputs and true values.
Exploration of CNN internal parameters is automatized.
Error is quantified with Mean Absolute Error: MAE
Training database:
Each entry is synthetized with the sum of 1 to 5 contributions
~ 1 000 000 entries
Outputs of CNN
Sparse densenet: model developed by Park et al.
LeNet: first simple CNN
Optimization of CNN internal parameters
MAE on major peak position
MAE on major peak width

## Slide 8
Testing CNNs
 | Sparse densenet | LeNet
MAE on major peak position | 0.09 | 0.25
MAE major peak width | 0.02 | 0.05
MAE major peak amplitude | 0.01 | 0.03
MAE on total number of peaks | 0.03 | 0.1
Average fit time | 1.4x10-3 s | 1.1x10-4 s
Test database:
Similar database to training
Distinct entries employed to evaluate performances on new cases
~ 150 000 entries
Example of test result
Almost perfect superposition of CNN result and true major peak
Statistical error over test database:
Similar results to Park et al. (1 200 000 entries training database)
Results obtained here (1 000 000 entries) training database

## Slide 9
Iterative application of CNN
Neural network as been developed and trained on the identification of one peak
It is applied iteratively to find several contributions in a spectrum
Good results but still errors
Almost perfect fit
CNN is applied 5 times to iteratively find the remaining major peak
CNN is applied 5 times to iteratively find the remaining major peak
+
Least square reduction fit initialized by CNN results to “polish” results
Average processing time: 0.21 s per spectrum
Average processing time: 2.22 s per spectrum

## Slide 10
Iterative application of CNN: statistical results
Polishing step improves fit quality
Even in most difficult cases (five contributions), average error remains low
Statistics over iterative fit quality were not evaluated by Park et al.
Distribution of R² obtained over 500 test spectra:
Good fits
Fits to be improved by polishing step
More good fits
Overall fit quality is evaluated through R² coefficient for total spectrum:
Less fits of too low quality
Iterative fit
Iterative fit + “polish”
Fit quality is sufficient when R² > 0,995 (empirical threshold)
Lower average error after polishing
Remaining contributions are more noisy and more sensitive to accuracy of previous fits
Mean Average Error for each peak parameter:
(only cases with two or five contributions)

## Slide 11
Results on experimental measurements
Total fit time (50 spectra): 4 min
Measurement of Pb 4f:
Filtering noisy experimental data
4f 5/2
4f 7/2
Evolution of first peak contribution:
Laser on
Laser off
Two contributions found for both peaks: need of further optimization ?

## Slide 12
Results on experimental measurements
Measurement of I 3d
Filtering noisy experimental data
Total fit time (50 spectra): 4 min
3d 5/2
Need of better defined background ?
Evolution of two first peak contributions:
Laser on
Laser off

## Slide 13
Conclusion
Analysis of time resolved XPS measurements
Recursive procedure to find all contributions
Training of convolutional neural network to find the major contribution
Laser on
Laser off
Application to experimental measurements
Tracking of contribution properties over time