## Slide 1
Impact of measurement on aging ?
Accelerated pathways matching real world processes?
Increase statistics : simultaneous measurement of several samples  RotaImpact of measurement on aging ?
Accelerated pathways matching real world processes?
Increase statistics : simultaneous measurement of several samples  Rotating platform/Optical splitting & electrical switching
Study on CIGS with D Lincot to have a 4 Daniel paper
Coupled in-situ PL and IV characterization set-up developed for aging measurements
Proof of concept – Upcoming publication
Bayesian analysis – Upcoming publication
Machine Learning Techniques for High-throughout Analyses of TR-PES Measurements
Valorization Corner
Pending Issues
Convolutional Neural Network employed to fit XPS Spectra to quantify chemical states and Electronic properties
 Work 1 : Optimised CNN Architecture for accurate and precise analysis
   Work 2 : What are the actual mechanisms limiting the device’s lifetime ?
DISCUSSION / CONCLUSIONS
RESULTS
  Sparse DenseNet Fitting
Comparison of V and Δμ:
  PL only : all is fine (S1 and S2), slight degradation (S3)  stable material
  IV only : severe degradation (S1 and S3)  device is dead
  Coupled analysis: collection issues (mobility? interface?)
Pathway analysis:
  Shows similar pathways taken by all 3 samples (in case of minor deviation)
  Suggests decreasing RSH as the cause of performance degradation
Bayesian Approach:
  Validates decrease in RSH and shows an increase in interfacial trap density
PROCESS FLOW
Romaric Sallustre1,3,, Arthur Julien2,3
Jean-Baptiste Puel4, Philip Schulz2,3
IPVF Scientific Day 20th June 2024
  Bayesian Approach
The sequential subtraction technique accurately identifies the total number of peaks by iteratively applying regression to determine and subtract the largest-area peak from the spectrum until no significant peak features remain, ensuring precise and reliable peak determination while avoiding spectral distortions.
Basin-hopping optimization enhances by minimizing residual errors and improving the accuracy of spectrum decomposition into multiple peak functions.
1Université Paris Cité
2Institut Photovoltaïque d’Ile de France
3CNRS, Ecole Polytechnique, IPVF, UMR 9006
4EDF R&D
  Fitting Time: 43 sec for 100 spectra
Bayesian Optimization used to fit drift-diffusion model (SimSalabim).
Limits degradation to 6 key parameters.
(2 Shown)
Further fine tuning of fit required
1000 XPS spectra to analyze
Spectra Generation of Pb 4f 5/2 and I 4f 7/2
Time-Resolved X-ray Photoelectron Spectroscopy (TRXPS) generates a vast amount of data under time-resolved constraints. In such scenarios, machine learning algorithms enables accurate and efficient analysis of the extensive spectroscopic
Principles
Challenges
Notes: From here sort out which sample is which